## Slide 1
Ising superconductivity in gated MoS2
陈光毅
导师：陈剑豪
量子材料中心
17.12.15

## Slide 6
Ising superconductor (Zeeman-protected superconductor):
Intrinsic spin-orbit coupling induced effective Zeeman field with opposite directions in opposite corners (K, -K) locks the spins of Cooper pairs in an Ising-like fashion.
Effective Zeeman field prevents the alignment of the spin to in-plane magnetic fields and hence protects the superconducting state.
In-plane critical field Hc2 far beyond the Pauli paramagnetic limit.
Background
Notes: strongly protective when an effective Zeeman field from intrinsic spin-orbit coupling locks the spins of Cooper pairs in a direction orthogonal to an external magnetic field.

## Slide 7
Pauli limit:

## Slide 8
Bc2
Bp
Fulde-Ferrell-Larkin-Ovchinnikov state
Spintriplet superconductor
Spin-orbit coupling (SOC)
Spin-orbit scattering (SOS)
In some superconductors, the Pauli limit can be surpassed.

## Slide 10
the parallel-aligned spin configuration in Cooper pairs is not affected by Pauli paramagentism, and Bc2 can easily exceed Bp

## Slide 11
Pauli limit may be greatly exceeded through spin-orbit scattering, which randomizes electron spins and thus weakens the spin paramagnetic effect.
Several models have been developed to include the effects of Pauli spin paramagnetism and spin-orbit scattering, such as WHH theory and KLB theory.

## Slide 12
Device
EDLT: electric double-layer transistors
Ultra-high charge-carrier accumulation at the sample/electrolyte interface
Carriers are induced electrostatically without introducing extrinsic disorder
Science 338, 1193, 2012; Science 350, 1353, 2015
Nature Physics 12, 144, 2016

## Slide 13
MoS2
Beff
In-plane ISB in monolayer
SOC
Science 338, 1193, 2012; Science 350, 1353, 2015
Notes: Conduction-band electron pockets near the K and K' points in the hexagonal Brillouin zone of monolayer MoS2. Electrons in opposite K and K' points experience opposite effective magnetic fields Beff and –Beff, respectively (green arrows). The blue and red colored pockets indicate electron spins oriented up and down, respectively. (B) Side view (left) and top view (right) of the four outermost layers in a multilayered MoS2 flake. The vertical dashed lines show the relative positions of Mo and S atoms in 2H-type stacking. In-plane inversion symmetry is broken in each individual layer, but global inversion symmetry is restored in bulk after stacking. (C) Energy-band splitting caused by Beff. Blue and red bands denote spins aligned up and down, respectively. Because of 2H-type stacking, adjacent layers have opposite Beff at the same K points.

## Slide 14
Measurement and Results
Science 338, 1193, 2012; Science 350, 1353, 2015
n2D of up to 1014 cm−2

## Slide 15
Science 338, 1193, 2012; Science 350, 1353, 2015

## Slide 16
upper critical field of layered superconductors (or superconducting films)
Orbital contributions: coupling between the magnetic field and the electron momentum (current loops, vortex)
Anisotropic Ginzburg-Landau model (Lawrence and Doniach, 1970-71; adapted from M. Tinkham, Introduction to superconductivity)

## Slide 17
2D Tinkham model (Phys. Rev. 129, 2413, 1963)
Appliable condition for 2D Tinkham model: film thickness d <  (This condition can be easily satisfied since  ~ 500 Å)

## Slide 18
Science 338, 1193, 2012; Science 350, 1353, 2015
Notes: Magnetoresistance of sample D1 [with Tc(0) = 2.37 K near the onset of the superconducting phase] as a function of an in-plane magnetic field up to 37 T, at various temperatures. (B) Temperature dependence of Rs for sample D1 [with Tc(0) = 7.64 K] under different in-plane magnetic fields up to 32.5 T. The dashed lines in (A) and (B) indicate RN/2. Bc2 is determined as the intercept between dashed lines and Rs curves

## Slide 19
Nature Physics 12, 144, 2016

## Slide 20
When considering superconductivity in the 2D limit, interlayer coupling is set to zero. For strong spin-orbit scattering, the KLB fitting reduces to
Discussion

## Slide 21
KLB theory yield avery short SOS time of ~24 fs ，which is less than the total scattering time of 185 fs estimated from resistivity measurements at 15 K

## Slide 23
Bc2 enhancement is mainly caused by the intrinsic spin-orbit coupling in MoS2.
Intrinsic mechanism: Ising superconductivity
Zeeman type SOC
Rashaba type SOC

## Slide 25
Rashba type SOC
Spin splitting between majority and minority
Zeeman type SOC
Phys. Rev. Lett 113, 097001 (2014)
Spin splitting between majority and minority

## Slide 26
Typical example of Rashba type SOC:
Spin polarization of BiTeI by spin resolved ARPES
Nature Material 10, 521, 2011

## Slide 27
Typical example of Zeeman type SOC: TMDs
Crystalline field
Nature Physics 9, 563, 2013
D3h: M + C3v
M symmetry suppresses the Rashba term, because it avoids any electric polarity along the z axis required for Rashba spin splitting. (M is broken by gating)
The Zeeman term:
Invariant under
Spin polarization will be aligned along the z axis and becomes maximal/minimal along the -K directions.

## Slide 28
Science 350, 1353, 2015

## Slide 29
Rashba SOC alone could only enhance Hc2// slightly to 2 Hp.
Out plane Zeeman protection would be weakened with stronger Rashba SOC (strong gating, higher Tc).
Science 350, 1353, 2015;Nature Physics 12, 144, 2016
Competition between Rashba and Zeeman type SOC

## Slide 30
Related works
Nature Physics 12, 139, 2016

## Slide 31
Conclusion
Ising Superconductor
MoS2
Other materials and possible mechanism
Notes: The concept of the Ising superconductor is also applicable to other layered systems, where similar intrinsic SOC could be induced
by symmetry breaking.

## Slide 32
Thank you