## Slide 1
Chiral charge pumping in graphene deposited on a magnetic insulator
Yunyan Yao
20170512

## Slide 2
Time resolved measurements of dynamical magnetic processes
Spin wave excitation through spin polarized current
Optical spectroscopy on magnon Bose-Einstein condensates
About authors
University of Muenster(Germany)
Ural Division of RAS (Russia)
Sergej O. Demokritov
Group members:
Michael Evelt
Oleksandr Dzyapko
Vladislav E. Demidov
research area

## Slide 3
motivation
In spin pumping system, as the thickness of the metallic layer is reduced, additional interfacial effects must be considered. The different contributions may be identified by analyzing the symmetries of the voltage signal with respect
to different adjustable parameters
Single layer graphene(SLG)
Magnetic material(YIG)
Spin-wave induced interfacial effects
Microwave
field

## Slide 4
schematic
Thickness: YIG(5.1um),GGG(0.5mm);
Saturation magnetization of YIG with out-of-plane geometry 4πMS =1.75 kG ;
Gold contact patches indicated by (+) and (-) were used for electric measurements;
Spin waves are excited by microwave (MW) current flowing in one of the two narrow antennas, producing a local MW field;
The red arrows represent the precession of the exchange field following the magnetization dynamics

## Slide 5
Microwave & voltage measurement
temperature T=295 ±0.02 K, Ho > 2KOe;
Figure(b),keep f constant,vary Ho, characterizing the field-dependent excitation of spin waves in YIG;
number of small peaks
odd number constant spin wave modes resonance
a large absorption peak
FMR
Figre(c), measured voltage versus the applied magnetic field.
H- is the inversion of H+.
to MW absorption vs field, no visible change
to measured voltage vs field, change sign
?

## Slide 6
Symmetry breaking
the reference geometry
Rotation by 180◦ around the z axis
Mirroring with respect to the vertical xz plane (y → -y)

## Slide 7
Symmetry breaking
rotation by 180◦ around the normal to the film plane
Agree with the experimental finding
Rotation symmetry around the normal axis is existed

## Slide 8
Symmetry breaking
Mirroring with respect to the vertical xz plane (y → -y)
Not agree with the experimental finding
axial vector:A
(as H0,Ms)
mirror symmetry:
real vector:A
(as E,Ksw)
mirror symmetry:
the mirror reflection symmetry about the planes normal to the interface is broken

## Slide 9
FMR in YIG film
the frequency of the FMR in YIG films depends on whether the static magnetic field is parallel or antiparallel to the normal to the film surface
Aim : to check whether the observed nonequivalence is a characteristic feature of the YIG film itself;
systematically increases as H0 approaches 4πMS = 1.75 kG
depends on the direction (clockwise or counterclockwise
with respect to zˆ) of the magnetization precession.
mirror reflection symmetry about interface is broken

## Slide 10
Phenomenological model
based on the existence of a finite density of
screw dislocations in YIG
The voltage signal is related to the electromotive forces induced by the magnetization dynamics
exchange interaction couples the spins of itinerant electrons of SLG to the localized magnetic moments in YIG
The tilted exchange field translates the effect of the symmetry breaking in YIG into the electronic response of graphene
displacements of the carbon atoms
related to H0
related to Ksw

## Slide 11
Frequency dependence
predicts that the effect should exist only within a certain range of spin-wave frequencies around
the frequency dependence of V/Pabs exhibits a resonance-like behavior with the maximum at about 6 GHz
voltage is linearly proportional to the spin-wave intensity

## Slide 12
conclusions
experimentally observe a chiral charge pumping in YIG/SLG bilayers caused by the symmetry breaking at the YIG surface
The broken symmetry of the studied YIG film has been also experimentally confirmed by FMR measurements in bare YIG films
The developed theoretical model, predicts that the strength of the effect can be increased by making use of 2D conductors with a strong spin-orbital coupling, such as MoS2